| Venue / Campus | Tianjin Campus, China |
| --- | --- |
| Intakes / Durations | May – June (3 Weeks) / November – December (3 Weeks) |
| Training Hours | 128 hours (3 Weeks) |
| Course Outline |
| EASA 66 Module 6 | Contents | Theory (hours) | Practical (hours) |
| 6.1 | Aircraft materials - Ferrous | 17 |  |
| 6.1.1 7.6.2 | Characteristics, properties and identification of common alloy steels used in aircraft; Heat treatment and application of alloy steels; Testing of ferrous materials for hardness, tensile strength, fatigue strength and impact resistance. | 7 10 |  |
| 6.2 | Aircraft materials – Non Ferrous | 16 |  |
| 6.2.1 7.2.2 | Characteristics, properties and identification of common non-ferrous materials used in aircraft; Heat treatment and application of non-ferrous materials; Testing of non-ferrous material for hardness, tensile strength, fatigue strength and impact resistance. | 6 10 |  |
| 6.3 | Aircraft materials – Composite and Non-metallic | 10 |  |
| 6.3.1 6.3.2 6.3.3 | Composite and non-metallic other than wood and fabric: Characteristics, properties and identification of common composite and non-metallic materials, other than wood, used in aircraft; Sealant and bonding agents. The detection of defects / deterioration in composite and non-metallic material. Repair of composite and non-metallic material. Wooden structures: Construction methods of wooden airframe structures; Characteristics, properties and types of wood and glue used in aeroplanes; Preservation and maintenance of wooden structure; Types of defects in wood material and wooden structures; The detection of defects in wooden structure; Repair of wooden structure. Fabric Covering: Characteristics, properties and types of fabrics used in aeroplanes; Inspections methods for fabric; Types of defects in fabric; Repair of fabric covering. | 4 4 2 |  |
| 6.4 | Corrosion | 11 |  |
| 6.4.1 6.4.2 | Chemical fundamentals; Formation by, galvanic action process, microbiological, stress; Types of corrosion and their identification; Causes of corrosion; Material types, susceptibility of corrosion. | 6 5 |  |
| 6.5 | Fasteners | 16 |  |
| 6.5.1 6.5.2 6.5.3 6.5.4 | Screw threads Screw nomenclature; Thread forms, dimensions and tolerances for standard threads used in aircraft; Measuring screw threads Bolts, studs and screws Bolt types: specification, identification and marking of aircraft bolts, international standards; Nuts: self locking, anchor, standard types; Machine screws: aircraft specifications; Studs: types and uses, insertion and removal; Self tapping screws, dowels. Special bolts removal method: riveting gun vibration method, anti-skid (cone) method, pliers method, platen removal method. Locking devices Tab and spring washers, locking plates, split pins, pal-nuts, wire locking, quick release fasteners, keys, cir-clips, cotter pins. Aircraft rivets Types of solid and blind rivets: specifications and identification, heat treatment | 4 4 4 4 |  |
| 6.6 | Pipes and Unions | 16 |  |
| 6.6.1 6.6.2 | Identification of, and types of rigid and flexible pipes and their connectors used in aircraft; Standard unions for aircraft hydraulic, fuel, oil, pneumatic and air system pipes. | 8 8 |  |
| 6.7 | Springs | 4 |  |
| 6.7.1 | Types of springs, materials, characteristics and applications. | 4 |  |
| 6.8 | Bearings | 4 |  |
| 6.8.1 | Purpose of bearings, loads, material, construction; Types of bearings and their application. | 4 |  |
| 6.9 | Transmissions | 20 |  |
| 6.9.1 6.9.2 6.9.3 | Gear types and their application; Gear ratios, reduction and multiplication gear system, driven and driving gears, idler gears, mesh patterns; Belts and pulleys, chains and sprockets. | 8 8 4 |  |
| 6.10 | Control Cables | 6 |  |
| 6.10.1 6.10.2 6.10.3 6.10.4 | Types of cables; End fittings, turnbuckles and compensation devices; Pulleys and cable system components; Bowden cables; Aircraft flexible control systems. | 1 2 2 1 |  |
| 6.11 | Electrical Cables and Connectors | 8 |  |
| 6.11.1 6.11.2 6.11.3 | Cable types, construction and characteristics; High tension and co-axial cables; Crimping; Connector types, pins, plugs, sockets, insulators, current and voltage rating, coupling, identification codes. | 2 2 4 |  |